SPUN POLE

General

Spun Concrete Transmission Pole is the result of technological expertise using centrifugal casting and spinning to produce a dense, durable concrete, slender & elegant Spun Poles.

Applications

- Concrete Spun Poles are used for applications like:

- L.T/H.T/EHV Transmission Poles/Towers.

- Street Yard lighting.

- Traffic signals.

- Overhead electrical traction poles for Railway electrification.

- Grid Sub-stations Structures.

- Telecommunication.

Advantages

Some of the superior features of Concrete Spun Poles are:

- Cost Saving.

- Easy Availability.

- Pilferage proof.

- Maintenance free.

- Easy to Handle & Transportation.

- Stronger & uniform.

- Better Aesthetic.

- Equal strength in all directions.

- Stay anchors are considerably reduced.

PSC

Pre-Stressed Cement Concrete Poles

PSC / PCC poles are cement concrete poles which are pre-stressed using steel wires to provide more structural strength.

### Key Raw materials

### Cement
High Tensile Wire
Galvanised Iron Wire
Stone Aggregate

Manufacturing process

(a)Check Casting Moulds for Dimensions, soundness, supports,     alignment and Cleanliness
(b) Pre-stressing of HT wires
(c) Concrete Mix as per approved drawing
(d) Casting
(e) Position, Nos. and Dimensions of Lifting Hooks
(f) De-Moulding and De-tensioning and
(g) Curing and
(h) Stacking and testing.

Advantages / Benefits of PSC poles

- Resistance to corrosion in humid and temperate climates and to erosion in desert areas.

- Fire resistant, particularly to grass and bush fires near the ground line.

- Easily installed in drilled holes in ground with or without concrete fill.

- Lighter because of reduced cross-section when compared with reinforced concrete pole.

- Clean and neat in appearance and requiring negligible maintenance for number of years, thus ideally suited for urban installations.

- Electric safety and Safe Earthing

- Flexible for all locations for erection

- Pre-stressed concrete pole are designed to meet or surpass regulatory guidelines for all types of projects and poles meet the standards of REC.

- Popular line supports in recent age.

- Greater mechanical strength.

- Has longer life.

- Permit longer spans than steel poles.

- Have Good outlook.

- Needs less maintenance.

- Good insulating properties.

- Steam curing process makes the product processing more durable and fast.

- Corrosion free.

APPLICATIONS

- Power Distribution via installation of transformer in PSC Pole

- Small Transformer installation

- Power Distribution

RCC

Reinforced concrete (RC) (also called reinforced cement concrete or RCC) is a composite material in which concrete's relatively low tensile strength and ductility are counteracted by the inclusion of reinforcement having higher tensile strength or ductility.

## Advantages of Reinforced Concrete

- Reinforced concrete has a high compressive strength compared to other building materials.

- Due to the provided reinforcement, reinforced concrete can also withstand a good amount tensile stress.

- Fire and weather resistance of reinforced concrete is fair.

- The reinforced concrete building system is more durable than any other building system.

- Reinforced concrete, as a fluid material, in the beginning, can be economically molded into a nearly limitless range of shapes.

- The maintenance cost of reinforced concrete is very low.

- In the structure like footings, dams, piers etc. reinforced concrete is the most economical construction material.

- It acts like a rigid member with minimum deflection.

- As reinforced concrete can be molded to any shape required, it is widely used in precast structural components. It yields rigid members with minimum apparent deflection.

- Compared to the use of steel in structure, reinforced concrete requires less skilled labor for the erection of the structure.

PROCESS OF INDUSTRY

- RECIVING OF RAW MATERIALS:

The unit requires Sand, Cement, Steel rods and wires to manufacture the poles.

- TESTING OF RAW MATERIALS:

The raw material received undergoes various testing methods to ensure the quality of the raw materials. The quality of Metal sand is tested by visual inspection, metal test and sieving test. Steel is tested by shear test. Cement is tested by finesse test and ash content test.

- Manufacturing Process of

9Mtr / 8Mtr long PSC Pole

The twin moulds is duly washed, shall be used for fixing P.C. Wires in moulds each 4mm. Wire is given proper tension to ensure that neither there is loosen P.C. Wire nor does it intermingle with other PC wires & GI Wire. The concrete is prepared by mixing given ratio of cement, jelly, M-Sand & water in a concrete mixture machine, is such that it meets requirement of concrete mix necessary. While filling the concrete in moulds, they are given sufficient vibrations by vibrators to ensure no gaps/wholes are left in casted poles. Poles so casted are left for steam curing for 14 hours. Poles are detensionized after obtaining proper strength, and removed from moulds, one by one by chain pulley blocks mounted on gantry crane. To ensure proper water curing poles are put in curing tanks & submerged in it for 15-20 days & thereafter stacked in open.

9Mtr/ 8Mtr long RCC Pole

The gauge is created within the twin moulds box then the concrete is prepared by mixing given ratio of cement, jelly, M-Sand & water in a concrete mixture machine, is such that it meets requirement of concrete mix necessary. Poles so casted are left for steam curing for 14 hours. Poles are then removed from moulds, one by one by chain pulley blocks mounted on gantry crane after obtaining proper strength. To ensure proper water curing poles are put in curing tanks & submerged in it for 15-20 days & thereafter stacked in open.

SPUN POLE

The mould box is duly washed and oiled partially gauge is created within the mould. Wires in moulds is each of 7mm. Wire is given proper tension to ensure that neither there is loosen P.C. Wire nor does it intermingle with other PC wires & GI Wire. The concrete is prepared by mixing given ratio of cement, jelly, M-Sand & water in a concrete mixture machine, is such that it meets requirement of concrete mix necessary. The concrete mixture is filled in the mould and tension is applied placing the mould on the roller bed for 20minutes. Pole is detensionized after obtaining proper strength, and removed from moulds, by chain pulley blocks mounted on gantry crane. Poles so casted are left for steam curing for 8 hours To ensure proper water curing poles are put in curing tanks & submerged in it for 18 days & thereafter stacked in open.